## Slide 1
  Land Reclamation - containment bunds filled with dredged materials (clays and silts)
  Underlain by thick holocene clay layer up to 30m in depth
  Difficulty to estimate the rate of settlement
Aerial view of land reclamation at the Port of Brisbane
(Ganesalingam et al. 2012a)
The Port of Brisbane

## Slide 2
Three Dimensional
Axisymmetric Consolidation
What is the rate of consolidation when three dimensions are considered?

## Slide 3
Samantha Thomas
Bachelor of Civil Engineering
Supervisor: Julie Lovisa
Quantifying the Rate of Three Dimensional Consolidation

## Slide 4: What is Consolidation?
Reduction in volume of a soil stratum due to an application of stress
H0
Clay (e0)
∆H
t = 0
H
Clay
(e0 - ∆e)
t =
GL
GL

## Slide 5: One Dimensional Consolidation
Rate described by Terzaghi’s (1925) differential equation:
where:
= vertical coefficient of consolidation

## Slide 6: Average Degree of Consolidation (U-T) Curves
One Dimensional Curves for a Singly and Doubly Drained Soil Strata
Singly Drained
Doubly Drained

## Slide 7: Doubly/Singly Drained Soil Strata
Doubly Drained Soil Strata
Singly Drained Soil Strata
Clay
Permeable Boundary
Permeable Boundary
Clay
Permeable Boundary
Impermeable Boundary
Hdr =
Hdr = H
H
H

## Slide 8: The objectives of this thesis were to:
Derive an analytical equation that quantifies the anisotropy of a sample;
Develop design charts of average consolidation curves (U-T curves) for three dimensional axisymmetric consolidation with varying radius to height ( ratios and analysing with respect to the one dimensional U-T curve.
Develop a functional three dimensional axisymmetric consolidation apparatus;

## Slide 9: Anisotropy
Refers to elastic properties that are dependent on the orientation of the sample
Horizontal permeability (kh) and vertical permeability (kv) observed
Anisotropy in the coefficient of consolidation (cv and ch)

## Slide 10: Objective: To develop a functional three dimensional axisymmetric consolidation apparatus
Schematic – Three Dimensional Axisymmetric Consolidation Apparatus

## Slide 11
Partial Differential Equation:
Where
Analytical Solution:
Where :
Objective: To derive an analytical equation that quantifies the anisotropy of a clay
(Lovisa et al. 2014)

## Slide 12: Objective: To develop design charts of average consolidation curves (U-T curves) for three dimensional axisymmetric consolidation with varying radius to height ( ratios
Average Degree of Consolidation Curves for Varying R/H Ratios (Lovisa et al. 2014)

## Slide 13: Modified Curve Fitting Parameters
 |  | Casagrande |  | Taylor |  | 
R/H x (Ch/Cv)0.5 | Domain | fC | T50 | fT | B | T90
 | 52.1 | 4 | 0.049 | 1.15 | 0.5 | 0.212
320 | 52.1 | 4.15 | 0.048 | 1.14 | 0.49 | 0.212
7 | 32 | 4.23 | 0.0424 | 1.17 | 0.48 | 0.1968
4 | 32 | 4.27 | 0.037 | 1.21 | 0.48 | 0.185
3 | 29 | 4.29 | 0.034 | 1.24 | 0.47 | 0.176
2 | 27 | 4.33 | 0.029 | 1.29 | 0.47 | 0.158
1.5 | 27 | 4.38 | 0.0247 | 1.32 | 0.47 | 0.1418
1 | 27 | 4.4 | 0.017 | 1.38 | 0.47 | 0.11
0.8 | 27 | 4.4 | 0.0143 | 1.4 | 0.47 | 0.0915
0.6 | 27 | 4.4 | 0.0103 | 1.41 | 0.47 | 0.0666
0.5 | 27 | 4.38 | 0.008 | 1.43 | 0.47 | 0.052
0.4 | 27 | 4.43 | 0.0059 | 1.39 | 0.47 | 0.0376
0.3 | 27 | 4.42 | 0.0038 | 1.37 | 0.47 | 0.0235
0.2 | 27 | 4.41 | 0.0019 | 1.34 | 0.47 | 0.0115
0.1 | 27 | 4.4 | 0.00055 | 1.3 | 0.47 | 0.003
Modified curve-fitting parameters (Lovisa et al. 2014)

## Slide 14: Modified Curve Fitting – Casagrande’s Method
Chart: Log(σv') (kPa)
| 0.15 | 6.54 | 12.92 | 25.7 | 48.44 | 96.73 | 193.32 | 386.49 | 772.83 | 1545.51 | 3090.88
Modified Coefficient of Consolidation | 0 | 0 | 0 | 101.869 | 136.0384 | 140.4265 | 143.1263 | 102.5428 | 54.1921 | 75.5968 | 62.2455
Unmodified Coefficient of Consolidation | 0 | 0 | 0 | 79.5738 | 78.4053 | 72.638 | 85.0474 | 47.8835 | 32.9551 | 52.0916 | 47.2494

## Slide 15: Verification with Experimental Data
Chart: Time Factor, T

## Slide 16: To Quantify Anisotropy
Average Degree of Consolidation Curves for Varying R/H Ratios (Lovisa et al. 2014)

## Slide 17: Quantifying Anisotropy in Coefficient of Consolidation
Chart: R/H x (Cv/Ch)0.5
| 320 | 7 | 4 | 3 | 2 | 1.5 | 1 | 0.8 | 0.6 | 0.5 | 0.4 | 0.3 | 0.2 | 0.1
 | 0.048 | 0.0424 | 0.037 | 0.034 | 0.029 | 0.0247 | 0.017 | 0.0143 | 0.0103 | 0.008 | 0.0059 | 0.0038 | 0.0019 | 0.00055
Quantifying Anisotropy using Modified Time Factors – Casagrande’s Method (Lovisa et al. 2014)
Chart: R/H x (Cv/Ch)0.5
| 320 | 7 | 4 | 3 | 2 | 1.5 | 1 | 0.8 | 0.6 | 0.5 | 0.4 | 0.3 | 0.2 | 0.1
 | 0.212 | 0.1968 | 0.185 | 0.176 | 0.158 | 0.1418 | 0.11 | 0.0915 | 0.0666 | 0.052 | 0.0376 | 0.0235 | 0.0115 | 0.003
Quantifying Anisotropy using Modified Time Factors – Taylor’s Method (Lovisa et. al 2014)

## Slide 18: Quantifying the Horizontal Coefficient of Consolidation – Casagrande’s Method
Comparison between the Horizontal Coefficient of Consolidation and Vertical Coefficient of Consolidation – Casagrande’s Method

## Slide 19: Scanning Electron Microscope
SEM Image – After Sample Preparation (Top View)
SEM Image - After Standard Oedometer

## Slide 20: Conclusions
Consideration of Three Dimensional Consolidation
Decreased Curve fitting domain from 60% for 1D to 30% for 3D
 | Advantages | Disadvantages
Casagrande’s Method | - No change to actual curve, just fitting procedure | -Use of modified curve fitting method has a large effect on the horizontal coefficient of consolidation obtained
Taylor’s Method | -Minimal difference in the coefficient of consolidation obtained using the modified method | Many coefficient of consolidation values could not be quantified for early load increments

## Slide 21: Significance to the Geotechnical Community
TIME REDUCTION
COST REDUCTION
Ability to complete experimental procedure in a shorter period of time through the use of a 3D apparatus
  Allows the coefficient of consolidation to be determined quicker, and settlement calculation completed
Allows a more accurate estimate of the time of consolidation in field application due to the consideration of horizontal drainage
  A shorter time estimate allows works to be completed on the consolidating layer sooner, resulting in cost reduction.

## Slide 22: Any Questions?

## Slide 23: Poster

## Slide 24: References
Ganesalingam, D., Ameratunga, J., Scweitzer, G., Boyle, P. & Sivakugan, S. Anisotropy in the permeability and consolidation characteristics of dredged mud. ANZ 2012 Conference Proceedings. Ground Engineering in a Changing World: 11th Australia - New Zealand Conference on Geomechanics 2012a Melbourne, VIC, Australia pp. 752-757.
Lovisa, J., Thomas, S., Macdonald, S. & Sivakugan, N. (2014). "A Method to Determine ch using Three Dimensional Consolidation " ASTM Geotechnical Testing Journal.
Lovisa, J. & Sivakugan, N. "Tall Oedometer Testing: A Method to account for wall friction."

## Slide 25: Curve Fitting – Casagrande’s Method
Fits a point at 50% consolidation
Casagrande’s Log Time Method (using experimental results if 155 kPa loading increment)

## Slide 26: Curve Fitting – Taylor’s Method
Fits a point at 90% consolidation
Taylor’s Square Root of Time Method, (using experimental results of 618 kPa increment)

## Slide 27: Determining T50, 3D
Method 1:
Method 2:

## Slide 28: Falling Head Permeability Testing
Comparison Between the Coefficient of Consolidation obtained from Taylor’s and Casagrande’s method, and the direct determination of permeability.
Chart: Log σv'
| 2 | 5.66 | 9.32 | 16.64 | 29.67 | 57.34 | 112.68 | 223.35 | 444.7 | 887.41 | 1772.81
Casagrande's Method | 0 | 0 | 0 | 0.34808 | 0.82603 | 1.0935 | 2.5475 | 4.8486 | 8.1792 | 0 | 14.5977
Taylor's Method | 0 | 0 | 0 | 0 | 0 | 0 | 3.5378 | 3.35 | 3.3135 | 3.2178 | 3.5952
Direct Permeability Method | 0 | 0.79603 | 28.0549 | 21.0566 | 60.4578 | 53.447 | 46.6836 | 46.1374 | 45.8936 | 50.0432

## Slide 29: Sample Preparation – Tall Oedometer
Dial Gauge
Soil Sample
Pressure Tap
Base Drainage Valve
Surface Drainage Valve
Tall Oedometer Schematic
Tall Oedometer Apparatus

## Slide 30: Standard Oedometer
Time-settlement
monitoring
Rowe Cell
Lever Arm

## Slide 31: Is Wall Friction a Factor?
Sample Preparation
  77 mm wide specimen, 63 mm sample obtained, therefore wall friction not considered an issue
Three Dimensional Consolidation Apparatus
  Paper by Lovisa and Sivakugan – A method to account for wall friction
    indicates that for a doubly drained sample,
    3D Sample H/D = 1 – Friction is negligible

## Slide 32: Solving PDE – Three Dimensional Consolidation
Scaled variables with respect to r, z, t and u were introduced:
,
Resulting in
With a Domain

## Slide 33: Current Approaches
Analytical:
  Terzaghi and Rendulic (1937)
  Biot (1945)
Numerical

## Slide 34: Properties of Experimental Clay - Kaolinite
Specific Gravity (Gs) | 2.469
Plastic Limit (PL) (%) | 37.2
Liquid Limit (LL) (%) | 81.4
Linear Shrinkage (LS) (%) | 12
Plasticity Index (PI) (%) | 44.2
 | 2.469
Plastic Limit (PL) (%) | 37.2
Liquid Limit (LL) (%) | 81.4
Linear Shrinkage (LS) (%) | 12
Plasticity Index (PI) (%) | 44.2

## Slide 35: Further Experimental Observations - Creep
Comparison of Coefficient of Secondary Consolidation ( for three dimensional and one dimensional consolidation

## Slide 36: Compression/Recompression Index
Chart: log σv' (kPa)
| 2 | 5.66 | 9.32 | 16.64 | 29.67 | 57.34 | 112.68 | 223.35 | 444.7 | 887.41 | 1772.81 | 887.41 | 444.7 | 223.35 | 112.68 | 57.34 | 29.67 | 16.64 | 9.32 | 5.66
 | 3.6455 | 3.6381 | 3.5799 | 3.5568 | 3.4838 | 3.4068 | 3.2754 | 3.0555 | 2.7383 | 2.3791 | 1.9731 | 1.9832 | 2.0212 | 2.0846 | 2.206 | 2.3054 | 2.3914 | 2.4682 | 2.5343 | 2.589
Void-log Curve for One Dimensional Consolidation
 | Compression Index (Cc) | Recompression Index (Cr)
1D, Vertically Cut Samples | 1.251 | 0.450
 | 1.562 | 0.296
 | 1.508 | 0.386
 | 1.223 | 0.321
1D, Horizontally Cut Samples | 0.587 | 0.319
 | 0.629 | 0.249
3D Samples | 1.046 | 0.147
 | 1.329 | 0.287
 | 1.262 | 0.419
Compression Index and Recompression Index Values for Experimental Results